Inspection & Testing Services

INSPECTION REPORT

External visual inspection – V-201 Air receiver / pressure vessel

Client

DEMO – Sample Process Plant (not a real client)

Demo Utilities Area

| Document control |  |
| --- | --- |
| Document number | ES/DEMO-EXT-2026-001 |
| Revision | Rev. 00 |
| Date | 10 Oct 2026 |
| Status | Issued |
| Inspection date | 10 Oct 2026 |
| Prepared by | Demo Inspector |
| Reviewed by | Demo Office Lead |
| Approved by | General Manager |

This document is confidential and is intended only for DEMO – Sample Process Plant (not a real client). It shall not be reproduced except in full without the written approval of EnvironmSafe.

1. DOCUMENT CONTROL

| Rev. | Date | Description | Prepared | Reviewed | Approved |
| --- | --- | --- | --- | --- | --- |
| 00 | 11 Oct 2026 | First issue | Demo Inspector | Demo Office Lead | General Manager |

CONTENTS

1.  DOCUMENT CONTROL

2.  SCOPE

3.  EQUIPMENT DETAILS

4.  METHOD

5.  RESULTS

6.  THICKNESS READINGS

7.  STATUS OF PREVIOUS FINDINGS

8.  FINDINGS AND PRIORITIES

9.  RECOMMENDATIONS

10.  CONCLUSION

11.  LIMITATIONS

12.  CERTIFICATES

13.  SIGN-OFF

14.  ANNEX – PHOTOGRAPHS

2. SCOPE

The scope of work covered the inspection of the equipment listed in this report in accordance with the referenced codes and the client's requirements.

This report records the external visual inspection of V-201 (Air receiver / pressure vessel) at Demo Utilities Area, which we carried out on 10 Oct 2026 with reference to API 510 (2022 edition). The inspection was witnessed by Demo Plant Engineer.

3. EQUIPMENT DETAILS

| Tag number | V-201 | Description | Air receiver / pressure vessel |
| --- | --- | --- | --- |
| Equipment type | Pressure vessel | Site / location | Demo Utilities Area – Compressor house |
| Manufacturer | Demo Fabricators | Model | AR-10 |
| Serial number | DF-5521 | Year built | 2012 |
| Service | Compressed air | Code of construction | ASME VIII-1 |
| Material | SA-516 Gr 70 | Capacity | 10 m³ |
| Design pressure | 12 bar | MAWP | 12 bar |
| Design temperature | 80 °C | Orientation | Vertical |
| Corrosion allowance (mm) | 3 |  |  |

4. METHOD

We carried out a close visual examination of the accessible external surfaces, welds, nozzles, supports and attachments, using hand lamps, mirrors and gauges where needed. Conditions found were recorded and photographed.

Checklist

| No. | Item | Result | Note |
| --- | --- | --- | --- |
| 1 | Nameplate present and legible | Yes |  |
| 2 | Shell / body free of visible corrosion, dents or bulges | No | Corrosion at bottom head |
| 3 | Supports, saddles, foundations and anchor bolts in good condition | No | Pitting at north leg |
| 4 | No leaks observed | Yes |  |

5. RESULTS

We carried out an external visual inspection and an ultrasonic thickness survey of the air receiver. External corrosion at the bottom head has progressed since the previous inspection. The drain valve has been replaced. The origin of the pitting at the north support leg could not be established from the as-found condition.

6. THICKNESS READINGS

| Point | Location | Nominal (mm) | t-min (mm) | Previous (mm) | Measured (mm) | ST rate (mm/y) | LT rate (mm/y) | Rem. life (y) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CML-01 | Top head | 12 | 8.2 | 11.6 (2025) | 11.5 | 0.100 | 0.060 | 33.0 |
| CML-04 | Bottom head | 12 | 8.2 | 10.6 (2025) | 10.1 | 0.500 | 0.219 | 3.8 |
| CML-05 | Drain nozzle | 7.1 | 4 | 6 (2025) | 5.8 | 0.200 | 0.139 | 9.0 |

ST = short-term rate (last two readings); LT = long-term rate (first and last readings). Remaining life uses the higher of the two rates.

7. STATUS OF PREVIOUS FINDINGS

| Ref. | Finding | Raised | Previous status | Status now | Our note |
| --- | --- | --- | --- | --- | --- |
| F-001 | External corrosion at bottom head | 10 Oct 2025 | Open | Open – deteriorated | Pitting deeper; coating breakdown now approx. 45 % of the head. |
| F-002 | Drain valve passing | 10 Oct 2025 | Open | Closed | Valve replaced by client in March 2026. |
| F-003 | Nameplate partly illegible | 10 Oct 2025 | Open | Open – unchanged | No change. |

8. FINDINGS AND PRIORITIES

| Ref. | Finding and location | Severity | Priority | Recommendation | Due |
| --- | --- | --- | --- | --- | --- |
| F-004 | Pitting at north support leg – North leg, 300 mm above base plate Scattered pitting up to an estimated 1.5 mm deep over an area of approx. 150 × 200 mm. | High | P1 | Clean to bare metal, measure pit depth and assess against API 579-1 Part 6; restore coating. | 10 Apr 2027 |
| F-005 | Earthing strap loose | Low | P3 | Re-tighten and test the earthing connection. | — |

P1: Action within 6 months.   P2: Action at the next shutdown and not later than the set due date.   P3: Continuous or routine attention.

9. RECOMMENDATIONS

Restore the coating system on the bottom head and support legs before the next inspection.

- F-004 (P1): Clean to bare metal, measure pit depth and assess against API 579-1 Part 6; restore coating.

- F-005 (P3): Re-tighten and test the earthing connection.

10. CONCLUSION

Fit for continued service with conditions

The equipment is considered fit for continued service subject to the conditions and recommendations stated in this report being completed by the dates given.

| Next inspection due | 10 Oct 2027 |
| --- | --- |
| Interval | 12 months |

11. LIMITATIONS

The internal surfaces were not examined within the scope of this inspection.

      
This report records the condition of the equipment as found on the date of inspection, within the scope and access available. Areas that were insulated, buried, inaccessible or not prepared were not examined unless stated. Where the origin of a condition cannot be established from the as-found condition, this is stated.

12. CERTIFICATES

| Certificate | Type | Issued | Issued by |
| --- | --- | --- | --- |
| ES-H-2026-001 | HYDRO | 10 Oct 2026 | Demo Office Lead |

13. SIGN-OFF

| Inspected by | Reviewed and issued by |
| --- | --- |
| Demo Inspector Senior Inspector · Cert. API 510 #00000 Date: 10 Oct 2026 | Demo Office Lead Date: 11 Oct 2026 |

14. ANNEX – PHOTOGRAPHS

| Figure 1 – Bottom head – external corrosion (F-001) | Figure 2 – Drain nozzle N5 with new valve (F-002) |
| --- | --- |
| Figure 3 – Nameplate (F-003) | Figure 4 – Pitting at north support leg (F-004) |